[image: image1.bmp]Concrete Test Results – Completed Example

	Asset ID No.:
	12345

	Bridge Project:
	HWY XX over XXX River

	Location:
	Sometown

	Contract #:
	2222/08

	Contractor:
	ABC Contracting

	Concrete Supplier:
	XYZ Concrete

	Plant Location:
	Concrete Town

	Consultant:
	AAA Consulting


	Date Tested:
	June 12, 2021

	Weather:
	Light Breeze, Cloudy
	  12 °C

	Tested By:
	Joe Tester

	Certification:
	 FORMCHECKBOX 
CSA    FORMCHECKBOX 
 ACI  
	Cert.#_12345__

	Date of Certification / Expiry:
	July 1, 2019
	July 1, 2022

	Cylinder Curing Facilities / Initial Temp:
	Curing Box
	17 - 23 °C

	Placing Method / Sampling Location
	Pump Truck
	Hose End

	Volume of Pour:
	80
	m3


	Specification

Requirements
	Concrete Class : HPC
	Strength:   45  MPa @  28 Days

	
	Slump (mm)
	Air Content (%)
	Number of Cylinder Sets Required

	
	Min.:
	90
	Max.:
	150
	Min.:
	5.0
	Max.:
	8.0
	Min of 1 set per :
	2
	Trucks                  or
	Min of 1 set per:
	20
	m3


	Pour Location
	Cylinder Identification

Labels*
	Delivery Ticket No.
	Load Amount
	Time
	Slump
	Air Content
	Unit Weight
	Temperature

	
	
	
	(m3)
	Batched
	Tested
	Off-Load
	(mm)
	(%)
	(kg/m3)
	Air (°C)
	Conc (°C)

	Deck pour over Pier #1.
	DS2-1,2,3,4
	1
	10
	20:00
	20:45
	20:50
	120
	6.5
	2400
	15
	16

	Deck pour over Pier #1.
	n/a
	2
	10
	20:30
	21:20
	21:25
	110
	6.8
	2395
	15
	16

	Deck pour over Pier #1.
	DS2- 5,6,7,8
	3
	10
	21:00
	21:40
	21:50
	125
	7.2
	2405
	14
	14

	Deck pour over Pier #1.
	n/a
	4
	10
	21:30
	22:15
	22:20
	130
	5.6
	2395
	14
	15

	Deck pour over Pier #2.
	DS4- 9,10,11,12
	5
	10
	22:00
	22:35
	22:45
	140
	5.8
	2400
	13
	13

	Deck pour over Pier #2.
	n/a
	6
	10
	22:30
	23:10
	23:15
	125
	6.7
	2400
	13
	17

	Deck pour over Pier #2.
	DS4-11,12,13,14
	7
	10
	23:00
	23:40
	23:45
	130
	7.0
	2405
	13
	16

	Deck pour over Pier #2.
	n/a
	8
	10
	23:30
	00:05
	00:10
	130
	6.5
	2402
	12
	15

	
	
	
	
	
	
	
	
	
	
	
	

	
	
	
	
	
	
	
	
	
	
	
	

	
	
	
	
	
	
	
	
	
	
	
	


[image: image2.png]


   Sketch of Test Cylinder Location:






Comments:


   Deck Section #’s:










Ticket No. 4 and 5 had 200 mL of superplasticizer added. 

      1            2          3           4            5







Superplasticizer used was EZY 123.
                        








            pg. _1_ of __1_
N





Abut #1





Abut #2





Pier #1





Pier #2








   * See Concrete Cylinder Coding Sheet for Suggested Cylinder Identification Label(s)
Concrete Test Results_Form Completion Example_Oct_2021










